NOTIFICATION

The following notification is being circulated in accordance with Article 10.6

| 1. | Notifying Member: THAILAND If applicable, name of local government involved (Article 3.2 and 7.2): |
| --- | --- |
| 2. | Agency responsible: Thai Industrial Standards Institute (TISI), Ministry of Industry Name and address (including telephone and fax numbers, email and website addresses, if available) of agency or authority designated to handle comments regarding the notification shall be indicated if different from above: WTO/TBT Enquiry Point and Notification Authority Thai Industrial Standards Institute (TISI), Ministry of Industry Tel.: (662) 202 3504 Fax: (662) 202 3511 E-mail: thaitbt@tisi.mail.go.th Website: http://www.tisi.go.th |
| 3. | Notified under Article 2.9.2 [X], 2.10.1 [ ], 5.6.2 [ ], 5.7.1 [ ], other [ ]: |
| 4. | Products covered (HS or CCCN where applicable, otherwise national tariff heading. ICS numbers may be provided in addition, where applicable): Flat steel products and semi-products (ICS 77.140.50) |
| 5. | Title, number of pages and language(s) of the notified document: Draft Thai Industrial Standard for Continuous Hot-dip 55% Aluminium/zinc-coated Cold-rolled Flat Carbon Steel of Commercial, Drawing and Structural Qualities (TIS 2228-2559 (2016)) (20 page(s), in Thai) |
| 6. | Description of content: The Thai Industrial Standards Institute (TISI) has proposed the draft compulsory Thai Industrial Standard for Continuous Hot-dip 55% Aluminium/zinc-coated Cold-rolled Flat Carbon Steel of Commercial, Drawing and Structural Qualities (TIS 2228-2559 (2016)). This standard covers flat carbon steel sheet 55% aluminium/zinc-coated by the continuous hot-dip process with 50 - 60% aluminium coating by mass, which is up to 4.0 mm in thickness and 1 500 mm in wideness. The coverage of standard includes scope; terms and definitions; coating, surface treatment, types and grades; dimensional tolerance; chemical composition; mechanical properties; requirements; marking and labelling; sampling and criteria; and test methods. |
| 7. | Objective and rationale, including the nature of urgent problems where applicable: Safety |
| 8. | Relevant documents: ISO 9364 : 2011 - Continuous hot-dip 55% aluminium/zinc alloy-coated steel sheet of commercial, drawing and structural qualities ISO 16163 : 2012 - Continuously hot-dipped coated steel sheet products – Dimensional and shape tolerances ISO 1460 : 1992 - Metallic coatings-Hot dip galvanized coatings on ferrous materials Gravimetric determination of the mess per unit area JIS G 3321-2007(2010) - Hot-dip 55% aluminuim-zinc alloy-coated steel sheet and strip TIS 2172-2556(2013) - Metallic materials - Tensile testing - Part 1: Method of test at room temperature |
| 9. | Proposed date of adoption: To be determined Proposed date of entry into force: To be determined |
| 10. | Final date for comments: 60 days from notification |
| 11. | Texts available from: National enquiry point [X] or address, telephone and fax numbers and email and website addresses, if available, of other body: WTO/TBT Enquiry Point and Notification Authority Thai Industrial Standards Institute Tel: (66 2) 202 3504 Fax: (66 2) 202 3511 E-mail: thaitbt@tisi.mail.go.th Website: http://www.tisi.go.th https://members.wto.org/crnattachments/2019/TBT/THA/19_3912_00_x.pdf |