NOTIFICATION

Corrigendum*

The following communication, dated 26 July 2019, is being circulated at the request of the delegation of Thailand.

_______________

This corrigendum is to inform that the information contained in Thailand's notification G/TBT/N/THA/551, circulated on 18 July 2019, should be corrected as follows:

1)	Amend its title from "Draft Thai Industrial Standard for Continuous Hot-dip 55% Aluminium/zinc-coated Cold-rolled Flat Carbon Steel of Commercial, Drawing and Structural Qualities (TIS 2228-2559 (2016))" to "Thai Industrial Standard for Continuous Hot-dip 55% Aluminium/zinc-coated Cold-rolled Flat Steel (TIS 2228-2559 (2016))".

2)	Under item 6 (Description of content) should read:

The Thai Industrial Standards Institute (TISI) has proposed to enforce the Thai Industrial Standard for Continuous Hot-dip 55% Aluminium/zinc-coated Cold-rolled Flat Steel (TIS 2228-2559 (2016)) as a compulsory standard.

This standard covers flat carbon steel sheet 55% aluminium/zinc-coated by the continuous hot-dip process with 50 - 60% aluminium coating by mass, which is up to 4.0 mm in thickness and 1 500 mm in wideness.

The requirements (surface treatment; types and grades; dimensional tolerance; chemical composition; mechanical properties; marking and labelling; sampling and criteria; and test methods) shall be in accordance to TIS 2228-2558 (2015); except the scope and item 2.1 of definitions; it shall follow as stated in the Notification of Ministry of Industry No. 4973 (B.E. 2560) Issued under the Industrial Product Standards Act B.E. 2511(1968): Amending Thai Industrial Standard for Continuous Hot-dip 55% Aluminium/zinc-coated Cold-rolled Flat Carbon Steel of Commercial, Drawing and Structural Qualities (TIS 2228-2558 (2015)) (Amendment No. 1)".

3)	Item 8 (Relevant documents) should read:

- TIS 2228-2558 (2015) Thai Industrial Standard for Continuous Hot-dip 55% Aluminium/zinc-coated Cold-rolled Flat Carbon Steel of Commercial, Drawing and Structural Qualities

4)	Add one more full text which is the above-mentioned Notification of Ministry of Industry.

https://members.wto.org/crnattachments/2019/TBT/THA/19_4194_00_x.pdf

__________