NOTIFICATION

The following notification is being circulated in accordance with Article 10.6

| 1. | Notifying Member: UGANDA If applicable, name of local government involved (Article 3.2 and 7.2): |
| --- | --- |
| 2. | Agency responsible: Uganda National Bureau of Standards Name and address (including telephone and fax numbers, email and website addresses, if available) of agency or authority designated to handle comments regarding the notification shall be indicated if different from above: |
| 3. | Notified under Article 2.9.2 [X], 2.10.1 [ ], 5.6.2 [X], 5.7.1 [ ], other [ ]: |
| 4. | Products covered (HS or CCCN where applicable, otherwise national tariff heading. ICS numbers may be provided in addition, where applicable): Hydraulic road binders; Quicklime, slaked lime and hydraulic lime, other than calcium oxide and hydroxide of heading 28.25 (HS 2522); Portland cement, aluminous cement, slag cement, supersulphate cement and similar hydraulic cements, whether or not coloured or in the form of clinkers (HS 2523); Cement. Gypsum. Lime. Mortar (ICS 91.100.10) |
| 5. | Title, number of pages and language(s) of the notified document: DUS DEAS 981:2019, Hydraulic road binders ― Composition, specifications and conformity criteria, First Edition. (20 page(s), in English) |
| 6. | Description of content: This Draft Uganda Standard applies to hydraulic road binders produced in a factory and supplied ready for use in road bases, sub-bases, capping layers, and soil stabilization or soil improvement. It specifies the mechanical, physical and chemical requirements for hydraulic road binders, together with the conformity criteria and evaluation procedures to be applied by the manufacturer. The stabilized road bases, sub-bases, capping layers, and soil stabilization or soil improvement by application of this hydraulic road binder shall comply with the requirements of BS 1924-1 Stabilized materials for civil engineering purposes ― Part 1: General requirements, sampling, sample preparation and tests on materials before stabilization and BS 1924 -2 Stabilized materials for civil engineering purposes ― Part 2: Methods of tests for cement-stabilized and lime–stabilized materials. |
| 7. | Objective and rationale, including the nature of urgent problems where applicable: Consumer information, labelling; Prevention of deceptive practices and consumer protection; Protection of human health or safety; Protection of the environment; Quality requirements; Harmonization; Reducing trade barriers and facilitating trade |
| 8. | Relevant documents: DD ENV 13282:2000, Hydraulic road binders ― Composition, specification and conformity criteria EAS 18-1 Cement ― Part 1: Composition, specification and conformity criteria for common cements EAS 18-2 Cement ― Part 2: Conformity evaluation EAS 148-1 Methods of testing cement ― Part 1: Determination of strength EAS 148-2 Methods of testing cement ― Part 2: Chemical analysis of cement EAS 148-3 Methods of testing cement ― Part 3: Determination of setting time and soundness EAS 148-4 Methods of testing cement ― Part 4: Determination of the chloride, carbon dioxide and alkali content of cement EAS 148-5 Methods of testing cement ― Part 5: Pozzolanicity test for pozzolanic cements EAS 148-6 Methods of testing cement ― Part 6: Determination of fineness EAS 148-7 Methods of testing cement ― Part 7: Methods of taking and preparing samples of cement EN 413-1 Masonry cement ― Part1: Specification EN 459-1 Building lime ― Part 1: Definitions specification and conformity criteria EN 459-2 Building lime ― Part 2: Test methods |
| 9. | Proposed date of adoption: March 2020 Proposed date of entry into force: Upon declaration as mandatory by the Minister for Trade, Industry and Cooperatives |
| 10. | Final date for comments: 60 days from notification |
| 11. | Texts available from: National enquiry point [X] or address, telephone and fax numbers and email and website addresses, if available, of other body: https://members.wto.org/crnattachments/2019/TBT/UGA/19_3793_00_e.pdf |